Welding Quality Control Plan (WQCP) Requirements 
in Accordance with “Welding Quality Control”

When required in contract documents, each Welding Quality Control Plan (WQCP) shall include the following items, as determined by the Engineer.  The WQCP shall be divided into the designated sections with each revision and addendum clearly annotated and numbered as shown below.  Each welding and NDT firm shall have separate sections for each firm.

# Organization

- The name of the welding firm.

- Name of QCM hired by Contractor, if applicable.

- Name of Quality Control Inspection firm hired by Contractor, if applicable.

- Name of NDT firm hired by Contractor, if applicable.

- Organizational chart showing the QCM, all subcontractors performing welding, QC firms and personnel, and NDT firms and personnel.

# Qualifications / Certifications

- Copy of AISC Certification, if applicable.

- Name, qualifications, and copies of certifications for the following individuals:

- QCM, if applicable.

- QC Inspectors

- Assistant QC Inspectors

- Copies of   qualification records for welders, welding operators, and tack welders for each welding process and position that will be used, and the joint detail. Certifications shall list the filler metals used, test position, base metal and thickness, tests performed, and the witnessing authority.  The submitted documentation shall be approved by the Engineer prior to any project welding being performed by a welder or welding operator.

- A master list of qualified welders that will document the welders and welding operators name, ID, the qualified welding process, welding position, and the date for each individual qualification and person qualified.

- The written description of the Contractors process for maintaining and providing the Engineer a current master list of qualified welders and welding operators that documents the names of each welder with the process, position, and date qualified as described in item “9” above.

# QC Procedures

- The methods and frequencies for performing all required visual inspections and documentation by which continuous visual inspection will not lapse for a period exceeding 30 minutes.

- A written description of the system and method of documentation the contractor will use for the identification and tracking of all welds, NDT, any required repairs, and re-inspection of non-conforming welds.  The contractors system shall include provisions for permanently identifying each weld and the person who performed the weld, NDT, inspection, and repair.

- Copies of the Quality Control forms to be used to include certificates of compliance, daily production logs, daily reports, weld repair tracking logs and visual inspection report forms.

- Documentation of the filler metal, flux, filler metal flux combination and shielding gas certifications to be used in the work and documentation of manufacturer’s recommended operating ranges.

- Authorized copy or original codebook for each of all AWS welding codes and the FCP, which are applicable to the welding being performed.

- Standard procedures for performing non-critical repair welds. Noncritical repair welds are defined as welds to deposit additional weld beads or layers to compensate for insufficient weld size and to fill limited excavations that were performed to remove unacceptable or NDT repairs, edge or surface discontinuities or undercut.

- The methods, procedures, and log to track rejected lengths of weld by welder, position, process, joint configuration, and piece number.

- Standard procedures for straightening members distorted by welding that do not require prior Engineer approval.

# WPS and PQR

- Pre-qualified Welding Procedure Specifications (WPS), if applicable.

- Documentation, when applicable, of Procedure Qualification Record (PQR) tests within the allowable period of effectiveness. Include all worksheets.

- Name of independent third party who performed or witnessed qualification tests, if applicable.

- Non-prequalified Welding Procedure Specifications (WPSs) supported by PQR testing.

- Documentation from the Engineer approving any deviation from standard joint details, code requirements or other contract documents.

# NDT Other Than Visual Procedures

- Written Practice of the NDT inspection personnel or firm.

- Name of certifying authority and outside Level III, if applicable.

- Names, qualifications, and documentation of certifications of NDT personnel to be used to include level of certifications and expiration date.

- List of NDT equipment, calibration procedures, frequencies and current qualification/calibration documentation of equipment to be used.

- Procedures, methods and frequencies for performing all required NDT as required by the contract documents to include minimum amounts required.

- Code of Safe Practices when Radiographic Testing (RT) is performed.

- A written description of the system for placing all identification and tracking information on each radiograph when Radiographic Testing (RT) is performed.

- Copies of NDT report forms to be used.

After final approval of the WQCP, amended WQCP, or addendum, the Contractor shall submit 7 copies to the Engineer of the approved documents.  A copy of the Engineer approved document shall be available at each location where welding is to be performed.

It is expressly understood that the Engineer's approval of the Contractor's WQCP shall not relieve the Contractor of any responsibility under the contract for the successful completion of the work in conformance with the requirements of the plans and specifications.  The Engineer's  approval shall not constitute a waiver of any requirement of the plans and specifications nor relieve the Contractor of any obligation thereunder; and defective work, materials, and equipment may be rejected notwithstanding approval of the WQCP.